From 860 to 219,292 cations: how data scale unlocks generative design of ionic liquids

Fuxing Lin (Hunan Institute of Engineering; ORCID 0000-0003-7588-6942)

> 第 6 篇手稿 v0.2（2026-08-15）。方法学主线：数据规模 × 生成范式 → 生成有效性

> 突破；三源交叉验证的诚实上限分析。与第 5 篇（JCIM 在投）的关系：第 5 篇在小

> 数据（860 阳/356 阴）上暴露"生成式设计"死结，本文证明死结的构成与解法。

Abstract

Generative design of ionic liquids (ILs) has been bottlenecked by data scarcity: a

character-level VAE trained on 860 cations produced chemically invalid species in

~40% of samples, and latent-space optimization collapsed onto the known optimum.

We decompose this bottleneck into two independent constraints — chemical validity

and property optimization — and show that only the former is a data-scale problem.

By assembling an experimental dataset of 6,177 unique ILs (2,838 cations / 592

anions; +227% over prior work) and a synthetically feasible space of 8.33 million

ILs (219,292 cations), we retrain three predictor families (GBM, HistGBM, MPNN)

under IL-disjoint cross-validation and a SMILES language model for generation.

Data expansion raises melting-point R² from 0.523→0.620 (GBM), 0.561→0.686

(HistGBM), 0.365→0.563 (MPNN) and lifts the generator's RDKit validity / charge

correctness from ~60% to 99.9%. The same expansion, however, does not yield

candidates predicted to beat the known optimum: two independent 8.3M-scale

predictors (ML model and chemical language model) agree that no IL in the virtual

space exceeds the experimental best (ln κ ≈ 0.64 for EMIM-DCA), with a

cross-predictor correlation of only 0.20 on conductivity. We conclude that (i)

chemical validity of IL generation is a solved problem at scale; (ii) surpassing

known property optima is bounded by the training distribution, not by generator

capacity; and (iii) the next bottleneck is experimental data with property labels,

not larger virtual libraries.

1. Introduction

Ionic liquids (ILs) — salts molten below ~100 °C — are the working fluids of choice

for a widening range of electrochemical and separation applications, from battery

electrolytes to CO₂ capture solvents. Because the cation–anion design space is

combinatorially vast (thousands of known ions, millions of synthetically feasible

pairs), machine learning has been used both to predict IL properties from

molecular structure and to generate new candidate structures. The predictive

direction has matured: with honest IL-disjoint validation, structure-based models

reach R² = 0.69–0.95 for conductivity, density and viscosity, and 0.36–0.56 for

melting point [1,2]. Transfer-learning and cross-domain frameworks extend this to

low-data regimes [6].

The generative direction, however, has hit a wall. In our previous work (paper 5,

ref [1]), a character-level VAE trained on 860 cations / 356 anions produced

chemically invalid SMILES in ~40% of samples (formal-charge errors, multi-fragment

species), and latent-space optimization converged back onto the known optimum

(EMIM-DCA) instead of discovering new optima. Two distinct bottlenecks were

conflated in that result:

(i) chemical validity — the generator must learn to emit charge-correct,

syntactically valid ion SMILES;

(ii) property optimization — even valid novel ions must be predicted to beat

the best known property values.

Here we separate these constraints experimentally. We expand the data on both

axes: an experimental set of 6,177 unique ILs (2,838 cations / 592 anions, +227%

over prior work, assembled from ILThermo and the Mendeley IL property dataset [4])

and a synthetically feasible virtual space of 8.33 million ILs (219,292 cations ×

38 anions) with two independent predictor families — the ILPE ML models [5] and

the ILBERT chemical language model [3]. We retrain our three predictors

(GBM/HistGBM/MPNN) under the same IL-disjoint protocol, replace the VAE with a

SMILES autoregressive language model trained on 150k cations (plus 30M unlabeled

IL-like SMILES for pre-training), and re-run combinatorial screening over 1.68

million novel cation–anion pairs. We show that (i) is solved at scale (99.9%

validity) while (ii) is not — a result we consider more informative than a

positive but fragile claim of "beating the optimum".

2. Results

2.1 Data expansion: 6,177 experimental ILs, 8.33M virtual ILs

Table 1. Data assets.

| Source | Type | Points / pairs | Unique ILs | Unique cations | Unique anions |
| --- | --- | --- | --- | --- | --- |
| ILThermo v2.0 (prior) | experimental | 88,661 | 1,891 | 860 | 356 |
| Mendeley tpp25ztzmb [4] | experimental | 39,928 | 5,220 | 2,381 | 375 |
| Merged experimental | — | ~129k | 6,177 | 2,838 | 592 |
| ILBERT virtual space [3] | predicted (chemLM) | 8,333,096 | 8,333,096 | 219,292 | 38 |
| ILPE virtual space [5] | predicted (ML) | 8,333,096 | 8,333,096 | 219,296 | 38 |
| ILBERT pre-train | unlabeled SMILES | 30,220,833 | — | — | — |

The merged experimental set more than triples prior IL coverage. The two virtual

spaces share the same combinatorial design (219k cations × 38 anions) but overlap

only 29.3% in ion identity after SMILES canonicalization, so their union exceeds

16 million unique ILs — and, importantly, they provide *two independent predictor

families* over a common design, enabling cross-predictor validation at scale.

2.2 Prediction gains from data scale (IL-disjoint)

All predictors were retrained on the merged experimental set under the protocol of

paper 5: IL-disjoint GroupKFold(5), 459 RDKit descriptors per ion pair (+T for

temperature-dependent properties), same loss scales. Table 2 and Fig. 2 report the

change from the paper-5 baselines (1,891 ILs).

Table 2. IL-disjoint R², paper5 (1,891 IL) → paper6 (6,177 IL).

| Property | GBM | HistGBM | MPNN |
| --- | --- | --- | --- |
| conductivity | 0.740 → 0.741 | 0.749 → 0.747 | 0.703 → 0.686 |
| density | 0.926 → 0.926 | 0.949 → 0.946 | 0.933 → 0.946 |
| viscosity | 0.809 → 0.791 | 0.846 → 0.834 | 0.759 → 0.759 |
| melting_point | 0.523 → 0.620 | 0.561 → 0.686 | 0.365 → 0.563 |

The largest and most consistent gains are on the melting point, whose IL count grew

~7-fold (570 → 3,945): +0.097 (GBM), +0.125 (HistGBM), +0.198 (MPNN). Viscosity

shows a small apparent drop (−0.018/−0.012/0.000). A decomposition shows this is

not a quality loss: among the 1,492 newly added viscosity ILs, 64% have a single

temperature point — pure cold-start cases under IL-disjoint CV. The subset of

paper-5 ILs retains R² = 0.808 (vs 0.809 before), and the new-IL subset alone

reaches R² = 0.728, i.e. the model generalizes to never-seen ILs rather than

degrading. This is evidence that data expansion buys extrapolation capacity on

single-point ILs — exactly the cold-start regime relevant to design.

2.3 Generator validity: model architecture × data scale

Table 3. Generator output quality.

| Model | Training cations | RDKit-valid | Charge = +1 | Novel cations (of 500k samples) |
| --- | --- | --- | --- | --- |
| paper5 char-VAE | 860 | ~60% | ~60% | few |
| char-VAE (this work) | 100,000 | 19.3% | 0.4% | 71 |
| char-VAE + β-anneal | 100,000 | 7.1% | 0.6% | — |
| SMILES LM (GRU) | 150,000 | 99.9% | 99.9% | 1,766 |

Scaling the training data 100-fold does not rescue the character-level VAE: its

KL term collapses to ~0 (posterior collapse), and validity actually degrades with

more data because the decoder collapses toward a mean sequence. The bottleneck was

architectural, not data. Replacing the VAE with an autoregressive SMILES language

model (GRU, teacher forcing, temperature/top-k sampling) trained on 150k

experimental-and-virtual cations raises RDKit validity and charge correctness to

99.9%, and 500k samples yield 1,766 cations that are novel with respect to the

entire 219k virtual library. **Chemical validity of IL generation is solved at

scale.**

2.4 Surpassing the known optimum: an honest limit

With validity solved, we asked whether novel cations can be predicted to beat the

known experimental optimum (EMIM-DCA, ln κ ≈ 0.64 at 298 K).

Unguided generation. Novel cations (1,766) paired with the 38 virtual anions give

67,108 candidates; our GBM/HistGBM predict ln κ < 0 for all of them (best −1.17).

The language model learned chemical plausibility, not property optimality —

its marginal distribution favors large, functionalized cations that are poor

conductors.

Guided generation. Fine-tuning the LM on top-scoring cations finds ln κ = 0.79

on the first round, above the 0.64 optimum; but strict (canonicalized) checks show

the top hits are known ILs (e.g. 1,3-dimethylimidazolium DCA), and the predictors

disagree systematically with the ILPE source.

Cross-predictor screen at 8.3M scale (Fig. 3). We merged the two independent

virtual spaces on canonicalized ion identity (633,780 ILs with valid conductivity

from both sources). The ILPE ML and ILBERT chemLM agree poorly on ln κ

(Pearson r = 0.20) and, crucially, **no IL receives a positive ln κ from both

sources** (ILPE max −0.24, ILBERT max +0.36; both below the 0.64 optimum). Two

independent, large-scale predictors therefore concur that the 8.3M virtual space

contains no candidate predicted to outperform the experimental best — not because

of generator failure, but because the predictors are bounded by their training

distribution.

Full combinatorial screen. We nevertheless screened all 2,838 × 592 = 1.68M

novel pairs in the experimental ion set with our retrained GBM/HistGBM (T = 298 K),

requiring agreed positive ln κ, room-temperature liquidity (Tm ∈ (180, 300) K) and

low viscosity (ln η < 5.5). After strict canonicalized novelty filtering and a

chemical sanity check (single-fragment anion, net charge −1), 16 candidates

survive with three-predictor agreement (Table 4, Fig. 4). The best, e.g.

1,3-diethylimidazolium DCA (ln κ = 0.51/0.43/0.46) and

1-vinyl-3-methylimidazolium DCA (0.46/0.69/0.75), are chemically reasonable,

room-temperature liquid, low-viscosity ILs with positive predicted conductivity in

all three independent predictors — but none exceeds the EMIM-DCA optimum

consistently.

**Table 4. Final candidates (three-predictor agreement, novel, chemically valid;

unique cations after canonicalization).**

| Cation (with DCA anion) | GBM ln κ | HistGBM ln κ | MPNN ln κ | Tm (K) | ln η |
| --- | --- | --- | --- | --- | --- |
| 1,3-diethylimidazolium | 0.511 | 0.427 | 0.463 | 269.6 | 3.05 |
| 1-vinyl-3-methylimidazolium | 0.461 | 0.688 | 0.751 | 281.5 | 3.28 |
| 1-ethylpyridinium | 0.417 | 0.609 | 0.436 | 284.1 | 3.41 |
| 1-ethylimidazolium | 0.386 | 0.359 | 0.712 | 277.3 | 3.20 |
| 1-methyl-3-propylimidazolium | 0.382 | 0.481 | 0.510 | 267.9 | 3.38 |
| 1-isopropyl-3-methylimidazolium | 0.308 | 0.410 | 0.550 | 286.2 | 3.78 |
| 1-ethyl-4-methylpyridinium | 0.303 | 0.353 | 0.551 | 297.8 | 3.61 |

Honest conclusion. Data scale solves chemical validity and prediction accuracy,

but does not make predictors "invent" property extrema outside their training

distribution. The road to surpassing known optima runs through property-labeled

experimental data, physical verification (DFT/MD), or active learning loops — not

through ever-larger virtual libraries.

3. Methods

Data. ILThermo v2.0 experimental records (prior work); Mendeley tpp25ztzmb [4]

(viscosity, melting point, CO₂ solubility, toxicity; cation/anion SMILES already

split); ILBERT virtual space + pre-training corpus [3] (Zenodo 14601320/15046370);

ILPE database [5] (Zenodo 3251661). Merged experimental set: 6,177 unique ILs;

descriptors computed per ion with RDKit (459 features), stored in

`il_descriptors_v2.csv`. Units standardized: T in K, viscosity in mPa·s (log

scale), density in g/cm³, conductivity in S/m (ln scale).

Predictors. GBM and HistGBM on RDKit descriptors; MPNN (3-layer message

passing, batch-encoded graphs, mean/sum/max readout) on ion graphs. Protocol:

IL-disjoint GroupKFold(5), identical to paper 5.

Generator. Character-level VAE (paper 5 architecture, baselines); SMILES

autoregressive GRU LM (emb 128, hidden 256, 2 layers), trained on 150k cations,

sampled with temperature 0.9–0.95 and top-k 15–20.

Cross-predictor validation. ILPE ML conductivity (S/m) filtered to positive

values and log-transformed; ILBERT ln κ used directly; merged on canonicalized

`cat|an` strings.

Combinatorial screen. 2,838 cations × 592 anions from the experimental set,

vectorized numpy feature construction, GBM/HistGBM scoring at T = 298.15 K,

filter: agreed ln κ > 0.2, Tm ∈ (180, 300) K, ln η < 5.5, novelty by canonicalized

exclusion of the 6,177 known ILs, chemical sanity (single-fragment anion, −1

charge).

Code and data. https://github.com/linfuxing123/IL-Property-ML, release v2.0.0

(https://doi.org/10.5281/zenodo.21941054).

4. Discussion

The central message is a decomposition, not a negative: **data scale solved one of

the two bottlenecks of generative IL design and provably cannot solve the other.**

Chemical validity — the failure that made paper 5's VAE output unusable — is now

at 99.9%, and the fix was architectural (autoregressive LM) enabled by scale

(large cation vocabulary, pre-training corpus). Prediction accuracy for

data-poor properties (melting point) improved substantially. But "beating the

known optimum" is bounded by the training distribution: two independent

8.3M-scale predictors agree that the virtual space contains no candidate predicted

to exceed EMIM-DCA, and our own three predictors converge on 16 novel, valid,

room-temperature-liquid candidates that are competitive but not superior.

Practical implications: (i) virtual-library inflation has diminishing returns for

property maxima; (ii) the binding constraint is now *property-labeled experimental

data (esp. conductivity/melting-point pairs for diverse ions) and physical

verification*; (iii) active learning — querying predictors where their

uncertainty is high, then validating experimentally — is the natural next step,

since our cross-predictor disagreement (r = 0.20) itself maps exactly the regions

where experimental confirmation would be most informative.

Limitations: predictors trained on 6,177 ILs carry their own error; the two

virtual spaces overlap only 29.3% (a strength for validation, a weakness for

direct comparison); the combinatorial screen uses only ions present in the

experimental set, so it cannot discover brand-new ion skeletons — only new pairs.

Generating genuinely new skeletons that also beat known optima will require the

experimental/physical loop above.

5. Data and Software Availability

All data, code, models, and the manuscript are publicly available at

https://github.com/linfuxing123/IL-Property-ML (release v2.0.0, archived at

https://doi.org/10.5281/zenodo.21941054). The archive contains the merged

experimental dataset (6,177 unique ILs), the ion-identity lists derived from the

8.33M-IL virtual space, all descriptor tables, the eight trained predictor models

(GBM/HistGBM × four properties), all scripts, and this manuscript with its

figures. Underlying public sources: ILThermo v2.0 (NIST); Mendeley tpp25ztzmb

[4]; Zenodo 7935198 (ILTransR), 14601320/15046370 (ILBERT), 3251661 (ILPE).

6. References (draft)

[1] Paper 5 (JCIM, under review) — inverse design under IL-disjoint validation.

[2] Paper 4 (ACS Sustainable Chem. Eng., under review) — GNN vs descriptors.

[3] Qiu, Y. et al. Large chemical language models for property prediction and

high-throughput screening of ionic liquids. Digital Discovery (2025).

[4] Dong, K.; Gao, J. The dataset of ionic liquid properties. Mendeley Data,

tpp25ztzmb (2025).

[5] The Ionic Liquid Property Explorer. Data 4, 88 (2019); Zenodo 3251661.

[6] Chen, G. et al. ILTransR: transfer learning for IL property prediction (2023).